|  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ***DESCRIPTION:*** | | | | | | | | | | | |
| Super breathable water-based paint for interiors based on vinyl. It is characterized by good hiding power. Easy to apply, it has excellent brushability and good yield. Ideal for indoor applications such as sheds and garages directly on concrete or after priming on plaster and old paints. | | | | | | | | | | | |
|  | | | | | | | | | | | |
| ***FEATURES:*** | | | | | | | | | | | |
| ASPECT | | | | Opaque | | | | | | | |
| OWN WEIGHT | | | | P1012.5: 1.62 Kg/l ± 0.05 at 20°C (KGP1014: 1.50 Kg/l ± 0.05 at 20°C) | | | | | | | |
| DRY RESIDUE | | | | 55 ± 0,5 % w/w | | | | | | | |
| WATER VAPOUR PERMEABILITY | | | | High | | | | | | | |
| DIRT GRIP | | | | Low | | | | | | | |
| COLOR | | | | White (Can be colored with Universal Dyes) | | | | | | | |
| DRYING  (data refer to 20°C and 65% R.H.) | | | | per coat: 6 hours  Full: 48 hours | | | | | | | |
| PRACTICAL PERFORMANCE | | | | 9-11 m2/L per coat  depending on the absorption of the substrate | | | | | | | |
| DILUTION | | | | 1st coat: add 30% drinking water  2nd coat: add 25% drinking water  Airless spray: Add between 30% and 40% drinking water. Recommended nozzles: LP419–LP519–LP619- LP421–LP521–LP621 | | | | | | | |
| PARAPHERNALIA | | | | brush | | | Roller | | | spray | |
| MEDIA | | | | civil plaster, plasterboard, fibre cement, stucco skimmed walls | | | | | | | |
|  | | | | | | | | | | | |
| ***APPLICATION*** | | | | | | | | | | | |
| **PREPARATION OF THE SUBSTRATE** | | | | | | | | | | | |
| The substrate must be healthy, dry, clean and consistent, free from moisture stains, traces of dirt, grease, mold, etc. Old, inconsistent or chalking paints should be removed by brushing or sanding the surface. Imperfections, cracks, peeling, must be eliminated and filled with appropriate putty. | | | | | | | | | | | |
|  | **NEW MEDIA** | | | | | **ALREADY PAINTED SUPPORTS** | | | | | |
| **PLASTER** | **HANDS** | **PLASTERBOARD** | | **HANDS** | **breathable or chalking** | | **HANDS** | **washable well anchored** | | **HANDS** |
| **BOTTOM** | **JANTAR** | **1** | **REFONDO** | | **1** | **JANTAR** | | **1** |  | |  |
| **FINISH** | **SUPERTRASPIRA** | **2** | **SUPERTRASPIRA** | | **1** | **SUPERTRASPIRA** | | **2** | **SUPERTRASPIRA** | | **2** |
|  | | | | | | | | | | | |
| **GENERAL WARNINGS** | | | | | | | | | | | |
| In order not to alter the typical breathable properties of the product, the amount of base dye must not exceed 20%. Keep the product cool and protect from frost. Do not apply the product at temperatures below 5° or above 30° centigrade, with relative humidity above 85% or on walls exposed to wind or sun. | | | | | | | | | | | |