|  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **DESCRIPTION:** | | | | | | | | | | | |
| Breathable water-repellent paint for interiors is characterized by excellent covering power and excellent white point. Easy to apply, does not require the application of any base product, has excellent brushability and good yield. Suitable for kitchens, bathrooms and in general for rooms subject to condensation. | | | | | | | | | | | |
|  | | | | | | | | | | | |
| **CHARACTERISTICS:** | | | | | | | | | | | |
| I WAIT | | | | Opaque | | | | | | | |
| SPECIFIC WEIGHT | | | | 1.61 Kg/l ± 0.03 at 20°C | | | | | | | |
| VOC (Directive 2004/42/EC): | | | | 1.29% - 20.00 g/litre | | | | | | | |
| WASHING RESISTANCE | | | | Average | | | | | | | |
| WATER VAPOR PERMEABILITY | | | | Average | | | | | | | |
| DIRT GRIP | | | | Low | | | | | | | |
| COLOR | | | | White (Colourable with Universal Dyes) | | | | | | | |
| DRYING  (data referred to 20°C and 65% RH) | | | | for covering: 6 hours  complete: 48 hours | | | | | | | |
| PRACTICAL YIELD | | | | 12-16 m2/L per coat  depending on the absorption of the support | | | | | | | |
| DILUTION | | | | 1st coat: add 35% drinking water, in the case of very powdery substrates add up to 100% drinking water  2nd coat: add 30% drinking water  Airless spray: add between 30% and 40% of drinking water. Recommended tips: LP419-LP519-LP619- LP421-LP521-LP624 | | | | | | | |
| TOOLS | | | | brush | | | roller | | | spray | |
| SUPPORTS | | | | civil plaster, plasterboard, fibre cement, stuccoed walls | | | | | | | |
|  | | | | | | | | | | | |
| **APPLICATION** | | | | | | | | | | | |
| **PREPARATION OF THE SUPPORT** | | | | | | | | | | | |
| The substrate must be healthy, dry, clean and consistent, free from damp stains, traces of dirt, grease, mold, etc. Old inconsistent or flaking paint must be removed by brushing or sanding the surface. Imperfections, cracks, flaking must be eliminated and filled with an appropriate filler. | | | | | | | | | | | |
|  | **NEW SUPPORTS** | | | | | **ALREADY PAINTED SUPPORTS** | | | | | |
| **PLASTER** | **HANDS** | **PLASTERBOARD** | | **HANDS** | **breathable or crumbling** | | **HANDS** | **washable well anchored** | | **HANDS** |
| **FUND** | **UNIQUE** | **1** | **UNIQUE** | | **1** | **UNIQUE**  **DILUTED FROM 50% 100%** | | **1** | **UNIQUE** | | **1** |
| **FINISH** | **UNIQUE** | **1** | **UNIQUE** | | **1** | **UNIQUE** | | **2** | **UNIQUE** | | **1** |
|  | | | | | | | | | | | |
| **GENERAL WARNINGS** | | | | | | | | | | | |
| In order not to alter the typical breathable properties of the product, the quantity of base dye must not exceed 20%. Store the product in a cool place and protect from frost. Do not apply the product at temperatures below 5° or above 30° centigrade, with relative humidity above 85% or on walls exposed to wind or sun. | | | | | | | | | | | |