|  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **DESCRIPTION:** | | | | | | | | | | | |
| Water-based wall finishing paint with excellent resistance to washing, slightly breathable for interiors, characterized by good covering power and good white point. It has excellent brushability and excellent yield, it differs from normal water-based paints for its particular velvety appearance, which enhances the quality of the finish, enhancing the environments where it is applied. Easy to apply, it allows both private and professional users to obtain finishes with a high aesthetic appearance. | | | | | | | | | | | |
|  | | | | | | | | | | | |
| **CHARACTERISTICS:** | | | | | | | | | | | |
| I WAIT | | | | Opaque | | | | | | | |
| SPECIFIC WEIGHT | | | | WHITE - 1.52 Kg/l ± 0.03 at 20°C  BASE BO - 1.44 Kg/l ± 0.03 at 20°C | | | | | | | |
| DRY RESIDUE | | | | 52 ± 0.5 % w/w | | | | | | | |
| WASHING RESISTANCE | | | | High | | | | | | | |
| WATER VAPOR PERMEABILITY | | | | Low | | | | | | | |
| DIRT GRIP | | | | Low | | | | | | | |
| COLOR | | | | White (Colourable with Universal Dyes) | | | | | | | |
| DRYING  (data referred to 20°C and 65% RH) | | | | for covering: 6 hours  complete: 48 hours | | | | | | | |
| PRACTICAL YIELD | | | | 9-13 m2/L per coat  depending on the absorption of the support | | | | | | | |
| DILUTION | | | | 1st coat: add 10% drinking water – Base BO 0%  2nd coat: add max 5% of drinking water – Base BO 0%  BO base to be used only after adding colorant.  Airless spray: add between 20% and 30% of drinking water. Recommended tips: LP419-LP519-LP619- LP421-LP521-LP624 | | | | | | | |
| TOOLS | | | | brush | | | roller | | | spray | |
| SUPPORTS | | | | civil plaster, plasterboard, fibre cement, stuccoed walls | | | | | | | |
|  | | | | | | | | | | | |
| **APPLICATION** | | | | | | | | | | | |
| **PREPARATION OF THE SUPPORT** | | | | | | | | | | | |
| The substrate must be healthy, dry, clean and consistent, free from damp stains, traces of dirt, grease, mold, etc. Old inconsistent or flaking paint must be removed by brushing or sanding the surface. Imperfections, cracks, flaking must be eliminated and filled with an appropriate filler. | | | | | | | | | | | |
|  | **NEW SUPPORTS** | | | | | **ALREADY PAINTED SUPPORTS** | | | | | |
| **PLASTER** | **HANDS** | **PLASTERBOARD** | | **HANDS** | **breathable or crumbling** | | **HANDS** | **washable well anchored** | | **HANDS** |
| **FUND** | **JANTAR** | **1** | **BACKGROUND** | | **1** | **JANTAR** | | **1** |  | |  |
| **FINISH** | **LABABLE** | **2** | **WASHABLE** | | **1 or 2** | **WASHABLE** | | **2** | **WASHABLE** | | **2** |
|  | | | | | | | | | | | |
| **GENERAL WARNINGS** | | | | | | | | | | | |
| In order not to alter the typical breathable properties of the product, the quantity of base dye must not exceed 20%. Store the product in a cool place and protect from frost. Do not apply the product at temperatures below 5° or above 30° centigrade, with relative humidity above 85% or on walls exposed to wind or sun. | | | | | | | | | | | |