|  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ***DESCRIPTION:*** | | | | | | | | | | | |
| Super breathable water-based paint for interiors based on vinyl. It is characterized by good covering power. Easy to apply, it has excellent brushability and a good yield. Ideal for interior applications such as sheds and garages directly on concrete or after priming on plaster and old paint. | | | | | | | | | | | |
|  | | | | | | | | | | | |
| ***CHARACTERISTICS:*** | | | | | | | | | | | |
| I WAIT | | | | Opaque | | | | | | | |
| SPECIFIC WEIGHT | | | | P1012.5: 1.62 Kg/l ± 0.05 at 20°C (KGP1014: 1.50 Kg/l ± 0.05 at 20°C) | | | | | | | |
| DRY RESIDUE | | | | 55 ± 0.5 % w/w | | | | | | | |
| WATER VAPOR PERMEABILITY | | | | High | | | | | | | |
| DIRT GRIP | | | | Low | | | | | | | |
| COLOR | | | | White (Colourable with Universal Dyes) | | | | | | | |
| DRYING  (data referred to 20°C and 65% RH) | | | | for covering: 6 hours  complete: 48 hours | | | | | | | |
| PRACTICAL YIELD | | | | 9-11 m2/L per coat  depending on the absorption of the support | | | | | | | |
| DILUTION | | | | 1 by hand: add 30% drinking water  2 by hand: add 25% drinking water  Airless Spray: Add 30% to 40% potable water. Recommended tips: LP419–LP519–LP619- LP421–LP521–LP621 | | | | | | | |
| TOOLS | | | | brush | | | Roller | | | spray | |
| SUPPORTS | | | | civil plaster, plasterboard, fibre cement, stuccoed walls | | | | | | | |
|  | | | | | | | | | | | |
| ***APPLICATION*** | | | | | | | | | | | |
| **PREPARATION OF THE SUPPORT** | | | | | | | | | | | |
| The substrate must be healthy, dry, clean and consistent, free from damp stains, traces of dirt, grease, mold, etc. Old inconsistent or flaking paint must be removed by brushing or sanding the surface. Imperfections, cracks, flaking must be eliminated and filled with an appropriate filler. | | | | | | | | | | | |
|  | **NEW SUPPORTS** | | | | | **ALREADY PAINTED SUPPORTS** | | | | | |
| **PLASTER** | **HANDS** | **PLASTERBOARD** | | **HANDS** | **breathable or crumbling** | | **HANDS** | **washable well anchored** | | **HANDS** |
| **FUND** | **JANTAR** | **1** | **REFONDO** | | **1** | **JANTAR** | | **1** |  | |  |
| **FINISH** | **SUPER TRASPIRA** | **2** | **SUPER TRASPIRA** | | **1** | **SUPER TRASPIRA** | | **2** | **SUPER TRASPIRA** | | **2** |
|  | | | | | | | | | | | |
| **GENERAL WARNINGS** | | | | | | | | | | | |
| In order not to alter the typical breathable properties of the product, the quantity of base dye must not exceed 20%. Store the product in a cool place and protect from frost. Do not apply the product at temperatures below 5° or above 30° centigrade, with relative humidity above 85% or on walls exposed to wind or sun. | | | | | | | | | | | |