|  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ***DESCRIPTION:*** | | | | | | | | | | | |
| Super breathable water-based paint for interiors. It is characterized by good covering power. Easy to apply, it has excellent brushability and good yield. Ideal for indoor applications such as sheds and garages directly on concrete or after priming on plaster and old paint. | | | | | | | | | | | |
|  | | | | | | | | | | | |
| ***CHARACTERISTICS:*** | | | | | | | | | | | |
| I WAIT | | | | Opaque | | | | | | | |
| SPECIFIC WEIGHT | | | | P1012.5: 1.62 Kg/l ± 0.05 at 20°C (KGP1014: 1.50 Kg/l ± 0.05 at 20°C) | | | | | | | |
| DRY RESIDUE | | | | 55 ± 0.5 % w/w | | | | | | | |
| WATER VAPOR PERMEABILITY | | | | High | | | | | | | |
| DIRT CATCHING | | | | Low | | | | | | | |
| COLOR | | | | White (Can be colored with Universal Dyes) | | | | | | | |
| DRYING  (data referred to 20°C and 65% RH) | | | | for recoating: 6 hours  complete: 48 hours | | | | | | | |
| PRACTICAL MAKE | | | | 9-11 m2/L per coat  depending on the absorption of the support | | | | | | | |
| DILUTION | | | | 1 by hand: add 30% drinking water  2 by hand: add 25% drinking water  Airless spray: add between 30% and 40% drinking water. Recommended nozzles: LP419–LP519–LP619- LP421–LP521–LP621 | | | | | | | |
| TOOLS | | | | brush | | | Roller | | | spray | |
| SUPPORTS | | | | civil plaster, plasterboard, fiber cement, plastered walls | | | | | | | |
|  | | | | | | | | | | | |
| ***APPLICATION*** | | | | | | | | | | | |
| **SUBSTRATE PREPARATION** | | | | | | | | | | | |
| The support must be healthy, dry, clean and consistent, free from humidity stains, traces of dirt, grease, mold, etc. Old inconsistent or flaking paint must be removed by brushing or sanding the surface. Imperfections, cracks, flaking , must be eliminated and filled with appropriate filler. | | | | | | | | | | | |
|  | **NEW SUPPORTS** | | | | | **SUPPORTS ALREADY PAINTED** | | | | | |
| **PLASTER** | **HANDS** | **DRYWALL** | | **HANDS** | **breathable or chalky** | | **HANDS** | **washable well anchored** | | **HANDS** |
| **BOTTOM** | **JANTAR** | **1** | **REFUND** | | **1** | **JANTAR** | | **1** |  | |  |
| **FINISH** | **SUPER TRASPIRA** | **2** | **SUPER TRASPIRA** | | **1** | **SUPER TRASPIRA** | | **2** | **SUPER TRASPIRA** | | **2** |
|  | | | | | | | | | | | |
| **GENERAL WARNINGS** | | | | | | | | | | | |
| In order not to alter the typical breathable properties of the product, the quantity of base color must not exceed 20%. Store the product in a cool place and protect from frost. Do not apply the product with temperatures lower than 5° or higher than 30° centigrade, with relative humidity higher than 85% or on walls exposed to wind or sun. | | | | | | | | | | | |