|  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **DESCRIPTION:** | | | | | | | | | | | |
| Breathable water-based interior wall paint, based on vinyl resin with a special broad-spectrum inhibitor against mold, fungi and algae, has a good white point, is easy to apply both with a roller and a brush, has excellent brushability, excellent coverage even on mold residues and excellent yield. Suitable for home and industrial environments such as kitchens, bathrooms, cellars, changing rooms and in general in rooms subject to the formation of mold and condensation. | | | | | | | | | | | |
|  | | | | | | | | | | | |
| **CHARACTERISTICS:** | | | | | | | | | | | |
| I WAIT | | | | Opaque | | | | | | | |
| SPECIFIC WEIGHT | | | | REONYX: 1.63 Kg/l ± 0.03 at 20°C | | | | | | | |
| DRY RESIDUE | | | | 58.00 p/p ± 5% | | | | | | | |
| WASHING RESISTANCE | | | | REONYX: LOW | | | | | | | |
| WATER VAPOR PERMEABILITY | | | | ONYX: HIGH | | | | | | | |
| DIRT GRIP | | | | LOW | | | | | | | |
| COLOR | | | | White (Colourable with Universal Dyes) | | | | | | | |
| DRYING  (data referred to 20°C and 65% RH) | | | | For recoating: 6 hours, full: 48 hours (data refers to 20°C and 65% RH) full: 48 hours | | | | | | | |
| PRACTICAL YIELD | | | | REONYX:10-14 m2/L per coat  depending on the absorption of the support | | | | | | | |
| DILUTION | | | | Add 1st coat: Brush application 30% drinking water, roller application 20% drinking water.  Add 2nd coat: Brush application 20% drinking water, roller application 20% drinking water.  Airless spray: add between 30% and 40% of drinking water. Recommended tips: LP419-LP519-LP619- LP421-LP521-LP624 | | | | | | | |
| TOOLS | | | | brush | | | Roller | | | spray | |
| SUPPORTS | | | | civil plaster, plasterboard, fibre cement, stuccoed walls | | | | | | | |
|  | | | | | | | | | | | |
| **APPLICATION** | | | | | | | | | | | |
| **PREPARATION OF THE SUPPORT** | | | | | | | | | | | |
| The substrate must be healthy, dry, clean and consistent, free from damp stains, traces of dirt, grease, mold, etc. Old inconsistent or flaking paint must be removed by brushing or sanding the surface. Imperfections, cracks, flaking must be eliminated and filled with an appropriate filler. | | | | | | | | | | | |
|  | **NEW SUPPORTS FREE FROM MOLD** | | | | | **ALREADY PAINTED SUPPORTS** | | | | | |
| **PLASTER** | **HANDS** | **PLASTERBOARD** | | **HANDS** | **WITH MOLD STAINS** | | **HANDS** | **washable well anchored** | | **HANDS** |
| **FUND** | **JANTAR** | **1** | **UNIQUE** | | **1** | **RE-23** | | **1** | **RE-23** | | **1** |
| **FINISH** | **REONYX** | **2** | **REONYX** | | **1** | **JANTAR** | | **1** | **JANTAR** | | **1** |
| **IF NECESSARY 2nd coat** | | | **REONYX** | | **2** | **REONYX** | | **2** |
|  | | | | | | | | | | | |
| **GENERAL WARNINGS** | | | | | | | | | | | |
| In order not to alter the typical breathable properties of the product, the quantity of base dye must not exceed 20%. Store the product in a cool place and protect from frost. Do not apply the product at temperatures below 5° or above 30° centigrade, with relative humidity above 85% or on walls exposed to wind or sun. | | | | | | | | | | | |