|  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **DESCRIPTION:** | | | | | | | | | | | |
| Water-repellent, breathable and anti-mold paint for interiors. It is characterized by good covering power and a good white point. Easy to apply, it has excellent brushability and a good yield. Suitable for kitchens, bathrooms and in general for rooms subject to the formation of condensation and mold. | | | | | | | | | | | |
|  | | | | | | | | | | | |
| **CHARACTERISTICS:** | | | | | | | | | | | |
| I WAIT | | | | Opaque | | | | | | | |
| SPECIFIC WEIGHT | | | | 1.58 Kg/l ± 0.03 at 20°C | | | | | | | |
| DRY RESIDUE | | | | 67 ± 0.5 % w/w | | | | | | | |
| WASHING RESISTANCE | | | | Average | | | | | | | |
| WATER VAPOR PERMEABILITY | | | | High | | | | | | | |
| DIRT GRIP | | | | Low | | | | | | | |
| COLOR | | | | White (Colourable with Universal Dyes) | | | | | | | |
| DRYING  (data referred to 20°C and 65% RH) | | | | for covering: 6 hours  complete: 48 hours | | | | | | | |
| PRACTICAL YIELD | | | | 11-13 m2/L per coat  depending on the absorption of the support | | | | | | | |
| DILUTION | | | | 1st coat: add 30% drinking water  2nd coat: add 25% drinking water  spray: add between 30% and 40% of drinking water. Recommended nozzles: LP419-LP519-LP619- LP421-LP521-LP624 | | | | | | | |
| TOOLS | | | | brush | | | roller | | | spray | |
| SUPPORTS | | | | civil plaster, plasterboard, fibre cement, stuccoed walls | | | | | | | |
|  | | | | | | | | | | | |
| **APPLICATION** | | | | | | | | | | | |
| **PREPARATION OF THE SUPPORT** | | | | | | | | | | | |
| The substrate must be healthy, dry, clean and consistent, free from damp stains, traces of dirt, grease, mold, etc. Old inconsistent or flaking paint must be removed by brushing or sanding the surface. Imperfections, cracks, flaking must be eliminated and filled with an appropriate filler. | | | | | | | | | | | |
|  | **NEW SUPPORTS** | | | | | **ALREADY PAINTED SUPPORTS** | | | | | |
| **PLASTER** | **HANDS** | **PLASTERBOARD** | | **HANDS** | **breathable or crumbling** | | **HANDS** | **washable well anchored** | | **HANDS** |
| **CLEANSING** | **RE23** | **1** | **RE23** | | **1** | **RE23** | | **1** | **RE23** | | **1** |
| **FUND** | **JANTAR** | **1** | **BACKGROUND** | | **1** | **JANTAR** | | **1** | **JANTAR** | | **1** |
| **FINISH** | **TITAN** | **2** | **TITAN** | | **1** | **TITAN** | | **2** | **TITAN** | | **2** |
|  | | | | | | | | | | | |
| **GENERAL WARNINGS** | | | | | | | | | | | |
| In order not to alter the typical breathable properties of the product, the quantity of base dye must not exceed 20%. Store the product in a cool place and protect from frost. Do not apply the product at temperatures below 5° or above 30° centigrade, with relative humidity above 85% or on walls exposed to wind or sun. | | | | | | | | | | | |