

**PURA12.5**



**PRODUCT TECHNICAL AND SAFETY DATA SHEET:**



**PURA**

**PITTURA NATURALE**

Code:

**PURA1**

**PURA2.5**

**P**

**URA5**

**PURA10**

|  |
| --- |
| ***DESCRIPTION:*** |
| Breathable water-based wall paint for interiors, based on acrylic resin with the addition of a special **NATURAL AND ECOLOGICAL** broad-spectrum inhibitor against mould, fungi and algae. It is characterized by excellent covering power and excellent whiteness. Easy to apply, it has excellent brushability and good yield. Suitable for kitchens, bathrooms and in general for rooms subject to the formation of mold and condensation.  **Product compliant with CAM certification.** |

|  |  |
| --- | --- |
| ***CHARACTERISTICS:*** | |
| I WAIT | Opaque |
| SPECIFIC WEIGHT | 1.52 Kg/l ± 0.03 at 20°C |
| DRY RESIDUE | 42 ± 0.5 % w/w |
| WASHING RESISTANCE | AVERAGE |
| WATER VAPOR PERMEABILITY | HIGH |
| DIRT CATCHING | Low |
| COLOR | White (Can be colored with Universal Dyes)  Associated with a tintometric system and can only produce pale colours. |
| DRYING (data referred to 20°C and 65% RH) | for recoating: 6 hours complete: 48 hours |
| PRACTICAL MAKE | 10-14 m2/L per coat  depending on the absorption of the support |
| DILUTION | 1st and 2nd coat: READY TO USE – **DO NOT ADD WATER**  In the case of very absorbent walls, 5-10% of MOLD NATURAL ADDITIVE can be added |
| TOOLS | Spray roller brush |
| SUPPORTS | civil plaster, plasterboard, fiber cement, plastered walls |

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ***APPLICATION*** | | | | | | | | |
| **SUBSTRATE PREPARATION** | | | | | | | | |
| The support must be healthy, dry, clean and consistent, free from humidity stains, traces of dirt, grease, mold, etc. Old inconsistent or flaking paint must be removed by brushing or sanding the surface. Imperfections, cracks, flaking , must be eliminated and filled with appropriate filler. | | | | | | | | |
|  | **NEW SUPPORTS FREE FROM MOLD** | | | | **SUPPORTS ALREADY PAINTED** | | | |
| **PLASTER** | **HANDS** | **DRYWALL** | **HANDS** | **WITH MOLD STAINS** | **HANDS** | **WASHABLE NOT CONTAMINATED** | **HANDS** |
| **BOTTOM** | JANTAR | 1 | PURE | 1 | RE-23 | 1 |  |  |
| **FINISH** | PURE | 2 | PURE | 1 | JANTAR | 1 | JANTAR | 1 |
| Only if necessary 3rd coat | | PURE | 2 | PURE | 2 |

|  |
| --- |
| **GENERAL WARNINGS** |
| In order not to alter the typical breathable properties of the product, the quantity of base color must not exceed 2%. Store the product in a cool place and protect from frost. Do not apply the product with temperatures lower than 5° or higher than 30° centigrade, with relative humidity higher than 85%. |